Airborne particle emission of a commercial 3D printer: the effect of filament material and printing temperature

Luca Stabile1, Mauro Scungio1, Giorgio Buonanno1,2, Fausto Arpino1, Giorgio Ficco1

1Department of Civil and Mechanical Engineering, University of Cassino and Southern Lazio, Cassino (FR), Italy.

2Queensland University of Technology, Brisbane, Australia.

corresponding author

Luca Stabile, PhD

Assistant professor

Department of Civil and Mechanical Engineering - University of Cassino and Southern Lazio (Italy)

Via Di Biasio 43, 03043 Cassino (FR)

Ph.  ++39(0) 7762993668

Fax.  ++39(0) 7762995502

Email: l.stabile@unicas.it

Practical implications

The study provides valuable and novel information on the emission of 3D printers in terms of airborne particles. 3D printing activities were found to emit a significant amount of ultrafine particles, whereas negligible emissions of larger particles were recognized. An effect of the printing temperature was also measured, since particle emission rates increase as function of the printing temperature. The study also highlights the possible contribution of 3D printing activities to the overall daily dose received by people working in microenvironments where 3D printers are run.

Abstract

The knowledge of exposure to the airborne particle emitted from 3D printing activities is becoming a crucial issue due to the relevant spreading of such devices in recent years. To this end, a low-cost desktop 3D printer based on fused deposition modeling principle was used. Particle number, alveolar-deposited surface area and mass concentrations were measured continuously during printing processes in order to evaluate particle emission rates and factors. Particle number distribution measurements were also performed to characterize the size of the emitted particles. Ten different materials and different extrusion temperatures were considered in the survey.

Results showed that all the materials investigated emit particles in the ultrafine range (with a mode in the 10-30 nm range), whereas no emission of super-micron particles was detected for all the materials under investigation. The emission was affected strongly by the extrusion temperature. In fact, the emission rates increase as the extrusion temperature raises. Emission rates up to 1×1012 particles min-1 were calculated. Such high emission rates were estimated to cause large alveolar surface area dose in workers when 3D activities run. In fact, a 40-min long 3D printing was found to cause doses up to 200 mm2.

# Keywords: 3D printers, ultrafine particles, emission, particle size distribution, emission rate, emission factor.

- Introduction

Exposure to airborne particles in indoor environments represents a leading issue in view of human health protection (Morawska et. al., 2013). Indoor micro-environments are usually considered as safe places, but this belief has no scientific basis since a number of researches confirmed that: i) outdoor-generated pollutants are not properly filtered by the building envelope (Ghirga and Pipere, 2012; Wardoyo et. al., 2012; Noh and Hwang, 2010; Stephens and Siegel, 2011; Liu and Nazaroff, 2001); ii) in presence of indoor particle sources the concentration levels in indoors strongly increase due to the reduced permeability of the building. The main particle sources in smoke-free indoor environments are: cooking activities (Buonanno et. al., 2009b; Buonanno et. al., 2011c; Stabile et. al., 2014; Stabile et. al., 2015b), biomass burning for heating purposes (Salthammer et. al., 2014; Spilak et. al., 2014), incense, candle and anti-mosquito product burning (Chuang et. al., 2012; See and Balasubramanian, 2011; Stabile et. al., 2012), resuspension phenomena due to walking or cleaning activities (Buonanno et. al., 2012a; Kim et. al., 2010; Corsi et. al., 2008; Fuoco et. al., 2015), terpene/ozone reactions forming secondary particles (Ishizuka et. al., 2010). In workplace micro-environments the range of sources is even wider, as example, welding activities (Buonanno et. al., 2011d; Moroni and Viti, 2009) and non-hot mechanical processes (e.g. ballistic impacts (Stabile et. al., 2013a) and grinding (Maynard and Zimmer, 2002)) were recognized as significant sources of sub-micron and super-micron airborne particles. Even cleaner workplace environments, such as (non-smoking) office buildings, where neither combustion or manufacturing processes are typically performed, present unexpected particle sources such as printers and photocopiers (Lee and Hsu, 2007; Schripp et. al., 2008; Destaillats et. al., 2008). He et. al. (2007) recognized that more than 60% amongst the 62 printers they tested could be considered emitters of ultrafine particles (i.e. particles smaller than 100 nm) showing emission rates up to 1.6×1011 part. min-1. A negligible emission rate in terms of PM2.5 was also estimated equal to 0.75 μg min-1. Hänninen et. al. (2010) showed that the exposure to ultrafine particles generated by laser printers is not negligible from an epidemiological point of view since risks associated with such exposure may exceed the threshold acceptable risk.

Recently, a “new way of printing” is getting a foothold in the market: the three-dimensional (3D) printing, i.e. the technology able to synthesize three-dimensional objects by means of additive manufacturing method (Glasschroeder et. al., 2015; Tibbits, 2015). Different printing techniques are currently available (fused deposition modeling, selective laser sintering, and stereo lithographic apparatus) but the most popular, cheapest and easiest to use is the fused deposition modeling (FDM). This technique is based on the extrusion of a thermoplastic material (supplied as a filament) through a heated extrusion nozzle head. The extruded material immediately cools down and then  hardens forming a solid layer. Thus the finished object is printed adding successive layers on the basis of the designed 3D models properly imported by the printer software. Even if such technology represents a promising opportunity in industrial and medical sectors (since functional prototypes, mobile robotics and tissue engineering applications can be easily shaped (Mota et. al., 2015; Raasch et. al., 2015; Stanton et. al., 2015; Singh et. al., 2015; de Obaldia et. al., 2015), the particle emission of 3D printers and related materials has been inadequately studied so far. This is a not trivial aspect considering that (i) 3D printers are not only used in controlled workplace environments, (ii) low-cost 3D printers are rapidly penetrating the market making them widely accessible for use in private homes and offices, (iii) physical and chemical composition of emitted particles may be significant different from those emitted by laser printers. Manufacturers typically provide data on the printing material safety highlighting that they comply with the regulation on the restriction of hazardous substances (European Parliament and Council of the European Union, 2011; Commission Regulation, 2010). Anyway, emission of dusts are expected since a local exhaust ventilation and good general extraction is suggested by the manufacturers to avoid reaching the dust occupational exposure limits (Occupational Safety and Health Administration, 2012).

Thermoplastic extrusion method per se has been recognized to emit various hazardous compounds (e.g. acrylonitrile, PAHs, VOCs) as a function of the material used (Chien et. al., 2010; Unwin et. al., 2013; Kim et. al., 2015; Steinle, 2015; Adams et. al., 1999; Lithner et. al., 2011; Azimi et. al., 2016). Anyway, early studies aiming to evaluate the emissions from 3D printers showed that a main pollutant to be investigated is represented by the airborne particles (Kim et. al., 2015; Steinle, 2015; Stephens et. al., 2013; Azimi et. al., 2016). Such researches, mostly performed on a limited number of materials and operating conditions (e.g. at a fixed extrusion temperature), reported significant emissions of sub-micron particles: they measured particle emission rates up to 1010 part. min-1 and 1011 part. min-1 for polylactic acid (PLA) and acrylonitrile-butadiene-styrene (ABS) materials, respectively.

To this purpose, the aim of this paper is the evaluation of the particle emission, and the main influence parameters, of a low cost 3D printer. An experimental analysis, aimed to measure number and mass particle emission rates and factors, was performed considering different materials and extrusion temperatures. Particle distribution measurements were also performed to characterize the size of the particles emitted.

- Material and methods

  - Site description

Measurements were performed from June 2015 to February 2016 in a room (volume 40 m3) of the European Accredited (EA) Laboratory of Industrial Measurements (LAMI), University of Cassino and Southern Lazio, Italy. Thermo-hygrometric conditions were continuously monitored in the room in order to maintain temperature and relative humidity values of 20±1 °C and 50±10%, respectively. The ventilation conditions were continuously maintained during the tests (doors and windows closed; mechanical ventilation turned off). The air exchange rate (AER) was also evaluated on the basis of the CO2 decay curve (He et al., 2004) through a CO2 probe based on the non-dispersive infrared absorption principle (Testo - Ambient CO2 probe; measuring range: 0-10000 ppm). Five measurements were performed in the room under investigation. In particular, the CO2 concentration decay in the room was measured for about 4 h as soon as people, typically occupying the laboratory, left the room: this sampling method guaranteed high and homogeneous CO2 concentrations inside the room. Windows and doors were kept close during the test. The average AER was measured equal to 0.22±0.07 h-1.

  - Particle source description

The 3D printer under investigation is a low-cost RepRap desktop 3D printer: in particular, a FDM 3D printer (Prusa i3, Prusa Research s.r.o., CZ) was used (Table 1). It allows small-scale manufacturing through heated thermoplastic extrusion technique and subsequent deposition of layers of fused materials. As most of the easy-to-use low-cost 3D printers, the device under investigation presents an open frame design since it has neither fume extraction system nor enclosure around the printing area, therefore possible emissions were released in the room.

Ten different materials were tested during the experimental campaign: PLA (polylactic acid), which is a biodegradable thermoplastic aliphatic polyester derived from corn starch, wood/copper/bamboo fibre-/powder-filled polylactic acids (referred as WOOD1, WOOD2, COPPER, BAMBOO, respectively, in Table 2), a softer and bendable PLA (referred as FLEX PLA in Table 2), a styrene-free copolyester (referred as CP in Table 2), a carbon fibre-filled styrene-free copolyster (referred as CARBON-CP in Table 2), NYLON, and a specially formulated thermoplastic polyurethane known as NINJAFLEX®. In Table 2 thermal and mechanical characteristics (as reported in the filament data-sheet) of the 10 materials investigated are summarized. 1.75 mm filament diameter was used in the experimental analysis.

A “Minion Dave” model was considered in the test as 3D object (Figure 1; width=2.38 cm, depth=2.27 cm, height=3.58 cm). A summary of the test performed was reported in Table 3. All the materials were tested at the same layer height (0.16 mm) and printing speed (16 mm s-1) and, thus, the same filament volume was used (2854 mm3). In Table 3 the printing temperatures were also summarized: different printing temperatures were tested for each material ranging from 180 to 240 °C. Test temperatures fell within the recommended ranges (Table 2) for most of the materials; temperatures higher than the suggested values were also tested (e.g. PLA was tested up to 240 °C even if the decomposition process is expected to start at lower temperatures (Al-Itry et. al., 2012; Mitchell et. al., 2009)).

A further test with no filament at 240 °C was also carried out in order to perform a “zero” test; in particular, three measurements were performed simulating the Minion Dave printing process not feeding the nozzle with the filament. The zero test is a key test since ultrafine particle emission is expected when metal surfaces are heated (Afshari et. al., 2005; Wallace et. al., 2015): therefore the nozzle heating process itself could lead to ultrafine particle emissions likely overestimating the printing process emission.

In order to properly compare the emission data of the investigated 3D printer when different materials are used, the same printing set up was considered. As an example, all the materials were printed with no heated plate in order to avoid artifacts due to the possible emission of the plate itself (this is also the reason why ABS material was not considered in the study). Moreover, printing process was performed with no “retraction” technique (i.e. “sucking” filament back up through the hot end in order to reduce filament oozing and depositing on the object under printing) since it was discouraged for certain materials. The authors recognize that such approach (i.e. using the same setup) could be not accurate in the view of the printing quality but it is a compulsory condition to provide a suitable discussion of the measurement data.

  - Experimental apparatus and quality assurance

In order to characterize the emission of the analyzed 3D printer, the following instruments were used:

- a butanol-based condensation particle counter (CPC 3775, TSI Inc.) able to measure the particle number concentration of particles >4 nm in diameter up to 1×107 part. cm-3 with 1-s sampling time;

- a light-scattering laser photometer (DustTrak aerosol monitor 8534, TSI Inc.) able to measure particle mass concentrations in terms of PM1, PM2.5, PM10 with 1-s sampling time;

- a scanning mobility particle sizer spectrometer (SMPS 3936, TSI Inc.) able to measure the particle number distribution in the sub-micron particle range. In particular, the SMPS is made up of an electrostatic classifier (EC 3080, TSI Inc.), which classifies particles according to their electrical mobility diameter, and a further CPC 3775 to count the classified particles, thus providing particle number size distribution. In the experimental analysis a sampling time of 135 s, an aerosol flow rate of 1.5 L min-1, and a sheath flow rate of 15 L min-1 were selected, then providing particle number size distributions in the 6-220 nm mobility diameter range;

- a nanoparticle surface area monitor (NSAM 3550, TSI Inc.) able to measure the total surface area of particles deposited in the alveolar and tracheobronchial regions of the lungs of a reference worker (Fissan et. al., 2007; Mokhtar et. al., 2013) with 1-s sampling time. In particular, the NSAM does not report the total surface area of particles suspended in the air but, rather, the total surface area of the particles that are deposited in the lung, in units of μm2 cm-3, applying the deposition fraction of particles as a function of their size as tabulated by the International Commission on Radiological Protection (1994). Major details on the principal of operation, simplified hypotheses, and comparison with SMPS are reported in Fissan et. al. (2007) and (Mokhtar et. al., 2013).

In order to guarantee the data quality assurance, the CPCs were calibrated in the European Accredited Laboratory at the University of Cassino and Southern Lazio comparing it to a TSI 3068B Aerosol Electrometer, using NaCl particles generated through a Submicrometer Aerosol Generator (TSI 3940) (Stabile et. al., 2013b; Buonanno et. al., 2009a). The NSAM and DustTrak were calibrated, for the specific aerosol under investigation, at the beginning of the experimental campaign by comparison with the SMPS 3936 (Mokhtar et. al., 2013) and the gravimetric method (which represents the reference method for particle mass concentration measurements, (Buonanno et. al., 2009a; Buonanno et. al., 2010)), respectively.

  - Methodology

In order to characterize the particle emission of the 3D printing process, particle number, alveolar-deposited surface area and mass concentration trends as well as particle number distribution measurements were performed during the printing process. The instruments (CPC 3775, DustTrak 8534, NSAM 3550 and SMPS 3936) were placed on a 1-m high desk at a distance of about 2 m from the printer (which was placed at the center of the room on a 0.6-m high desk). The following procedure was applied in the experiments: 10 min measurements of background concentrations followed by the measurements throughout the duration of the printing process, and then further 30–60 min of measurements after the printing had ceased to monitor the concentration decay. Three measurements were performed per each test defined in Table 3. From the concentration trends obtained through the CPC 3775, particle emission rates (ERs) and emission factors (EFs) were calculated. In particular, the ER was evaluated on the basis of the particle concentration trends applying the equation derived by He et. al. (2004):

(1)

where Cpeak and Cout represent the peak indoor concentration (whose results are reported in the result section; Table 4) and initial indoor particle concentration (which is assumed equal to the outdoor one), respectively,  is the average indoor concentration throughout the test,  is the average total removal rate, and Δt is time difference between initial (Cout) and peak (Cpeak) concentrations. This equation ignores the effects of particle dynamics such as condensation, evaporation and coagulation. Further examples of ER evaluation are reported in our previous papers (Stabile et. al., 2014; Fuoco et. al., 2014; Buonanno et. al., 2011d; Buonanno et. al., 2011c; Buonanno et. al., 2009b). Emission rate data for each test reported in the result section represent the mean values of the three measurements. Emission factors (EFs) as function of the length of the filament extruded during the printing time were also evaluated dividing the emission rate by the filament length and multiplying by the printing time. The emission factors were reported as function of the length of the filament since it is the key printing parameter (instead of mass which depends on the filament density).

Alveolar-deposited surface area concentration data were used to estimate the dose received by people working in the 40-m3 office supplied by a natural ventilation system. In fact, the measured averaged air exchange rate (0.22 h-1) is typical of public and private buildings not supplied by mechanical ventilation systems (d’Ambrosio Alfano et. al., 2012; Stabile et. al., 2015a; Stabile et. al., 2016). The alveolar surface area deposited dose (Buonanno et. al., 2011a; Buonanno et. al., 2011b) received during the 40-min long printing activity was evaluated for an adult performing a sedentary job (average value, between male-female, of inhalation rate for sitting activity, IR=0.47 m3 h-1; International Commission on Radiological Protection (1994)) as:

(2)

where SAlv_dep represents the average alveolar-deposited surface area concentration measured during the printing activity, and t is the printing activity length (40 min).

- Results and discussions

  - Particles’ concentration and distribution data

In Figure 2 an illustrative example of typical trends measured during the tests performed is reported. In particular, particle number, alveolar-deposited surface area and PM (PM1, PM2.5 and PM10) concentration trends are reported for one of three measurements performed for printing process using the BAMBOO filament at 220 °C. The particle number and alveolar-deposited surface area trends clearly highlight: a) the steady-state concentration typical of the background measurement period (about 2×104 part. cm-3 and 35 µm2 cm-3 for the measurement under investigation), b) the concentrations’ increase during the printing process up to a maximum value reached roughly at the end of the printing activity (about 1.10×105 part. cm-3 and 140 µm2 cm-3 for the measurement under investigation), c) the concentrations’ decay due to the particle source turning off. The particle number concentration trend showed a first increase of the concentration typical of the printer warming up period. To better highlight this early peak in concentration, particle number concentration trends of one of the three measurements of CP 220 °C and CP 230 °C tests are reported in Figure 3 since in those samplings higher warming period peaks were measured. Such phenomenon was recognized for all the filaments considered suggesting a not constant particle emission rate as also documented by Azimi et. al. (2016). A different behavior was recognized for the particle mass concentration trends: no effect of the printing process on the PM1, PM2.5 and PM10 concentrations in the room was measured, this could be due to the very small size of the particles emitted by the 3D printer as hereinafter documented (please see Figure 4).

In Figure 3 an example of the particle number concentration trend obtained for the zero test (no filament feeding) was also reported. In particular, a negligible increase in concentration was recognized when filament was not fed. This could be due to the small surface of the nozzle. Despite the zero test, all the other tests performed showed trends similar to those reported in Figure 2: in Table 4 (average) peaks of the particle number and alveolar-deposited surface area concentrations, if any, measured during the all the tests listed in Table 3 are reported. The authors point out that, even if for low emitting filaments the short-term particle concentration peak due to the printer warming up period resulted similar to (or even larger than) the peak typical of the printing process itself. The data reported in Table 4 represent the peaks due to the printing process (i.e. typically recognized at the end of the printing time), neglecting the possible short term peak due to the printer warming up period. Particle concentration results showed that, except for the tests PLA 180 °C, PLA 200 °C, PLA 210 °C, NYLON 220 °C and NINJAFLEX® 220 °C, all the tests performed were recognized to emit sub-micron particles. Peaks up to 1×106 part. cm-3 and 1×103 µm2 cm-3 were measured, whereas background concentrations in the ranges 2×103-3×104 part. cm-3 and 8-35 µm2 cm-3 were detected during the tests. Higher peaks were measured for higher extrusion temperatures suggesting a possible effect of the extrusion temperature on the emission rates/factors: details are hereinafter reported. The increase of particle number concentrations measured during the tests resulted sharper than the alveolar-deposited surface area ones. This could be explained by the typical (small) sizes of the particle emitted by the printing process. As an example, in Figure 4 the particle number distribution temporal evolution corresponding to the measurement reported in Figure 2 (i.e. one of the three measurements of the BAMBOO 220 °C test) is shown. The figure highlights the variation of the distribution’s mode and geometric standard deviation (GSD) due to the emission of fresh particles via printing process: a mode close to 100 nm (typical of an aged aerosol) was measured during the background period, whereas, particles in the ultrafine range were mostly emitted during the printing process. In particular, a mode in the 20-30 nm range was measured. During the decay, a negligible increase of the mode was measured: i.e. no significant coagulation phenomena were recognized during the decay. All the tests characterized by the emission of sub-micron particles presented particle number distribution evolutions similar to the one shown in Figure 4. Maximum standard deviations of the mode were within 20%, therefore, emission rates/factors can be calculated properly using the model reported in the Methodology section (equation 1). In Table 4 a summary of the particle number distribution characteristics (mode and GSD), averaged over the entire length of the printing period and over the three measurements, are reported for each test under investigation. Modes from 10 to about 30 nm were measured. No clear trends of the mode as function of the materials, extrusion temperatures and particle concentrations considered were recognized. On the contrary, narrower distributions (lower GSDs) were documented when higher amounts of particles were emitted: in fact, higher concentrations of particles in the 10-30 nm mode range make negligible the 100 nm background mode. Modes in the ultrafine ranges were also measured by Kim et. al. (2015) and Stephens et. al. (2013) during their characterization of PLA and ABS filament emissions: anyway, the use of instruments not able to measure particles smaller than 10 nm could have limited the emission characterization they proposed.

  - Particle emission rates and factors

On the basis of the particle number concentration trends and the equation (1), the emission rates were evaluated for each test performed. In particular, the average emission rate was estimated and the peak concentration data reported in Table 4 were considered in the evaluation of the emission rate calculation not considering the short term particle concentration increase during the warming period. In Table 5 the average emission rates (ERs, particles min-1) and factors (EFs, particles mm-1) obtained for each test performed, are reported as function of the extrusion temperature. ERs and EFs are clearly affected by the extrusion temperature: the higher the extrusion temperature the greater the particle emission. The temperature effect is better highlighted in Figure 5, where particle number emission rates were plotted as function of the extrusion temperature. As an example, the PLA, which represents the filament thoroughly used and investigated, when extruded at temperature lower than 220 °C does not show particle emission, whereas emission rates of 6.78×109, 2.47×1010, and 9.98×1010 particles min-1 (i.e. 2.26×108, 8.26×108, and 3.33×109 particles mm-1) were detected at 220 °C, 230 °C, and 240 °C, respectively. Such emission rates were roughly similar to the ones reported in previous papers (Kim et. al., 2015; Steinle, 2015; Stephens et. al., 2013) and larger than ones reported in Azimi et. al. (2016). Anyway, for a proper comparison, the possible effect of other printing parameters should be considered (e.g. extrusion speed, use of heated bed, etc.). Moreover, attention should be paid also to the different experimental apparatus used in the analyses: the abovementioned studies performed particle number concentration measurements down to 10 nm then likely underestimating the amount of the freshly-emitted particles smaller than 10 nm (please see Figure 4 and Table 4). The effect of the temperature for PLA filament could be addressed to the effect decomposition phenomena: such process is expected to start at temperature higher than 200 °C being massive at 300 °C (Al-Itry et. al., 2012; Mitchell et. al., 2009; Yang and Lin, 2009). These phenomena could partially explain the similar temperature effect recognized for the other materials, in fact, most of them are PLA-based filaments. In particular, the elevated temperature could lead to a higher vapor pressure of organic material which might promote the particle formation process (Jarmer et. al., 2004; Yang et. al., 2014). Actually, the PLA filament presents a quite low emission rate/factor when compared to the WOOD 2, COPPER, BAMBOO, CP and CP-CARBON filaments whose emission rates were larger than 1012 particles min-1 at 240 °C. Emission factors of NINJAFLEX® and FLEX PLA resulted quite similar to the PLA ones, whereas WOOD 1 ones were slightly larger. Finally, NYLON filament did not show emission for extrusion temperatures lower than 230 °C, whilst its emission at 230 °C and 240 °C resulted quite constant and slightly higher than 1×1011 particles min-1. The authors point out that, in order to provide a more exhaustive discussion on the effect of the extrusion temperature on the emission rates, a more detailed chemical characterization of the filaments’ materials should be performed. As an example, no information are provided by the manufacturer on the abovementioned “proprietary additivation” (Table 2) neither on the possible use of glue. The authors highlight that the emission rates measured for 3D printers are comparable to the ones typical of the most important indoor particle sources characterized by combustion phenomena such as cooking activities (Buonanno et. al., 2011c; Buonanno et. al., 2009b; Stabile et. al., 2015b; Stabile et. al., 2014) and candle/incense burning (Stabile et. al., 2012). Moreover, such emission resulted even larger than those typical of office printers (He et. al., 2007).

  - Surface area dose

In Table 6 average alveolar particle surface area doses received by an adult during a 40-min long 3D printing activity are reported. Adults performing a sedentary job in a 40-m3 office where a 3D printer is in operation were considered. Such scenario represents a typical office not supplied by mechanical ventilation systems (in fact a ventilation rate equal to 0.22 h-1 was measured as mentioned above). Values ranged from about 4 mm2, for low emitting tests (e.g. PLA at 220 °C), to 240 mm2, for the most emitting test (WOOD 2 at 240 °C), with several tests performed causing alveolar surface area dose larger than 50 mm2. This represents a significant dose taking into account that the daily average alveolar surface area dose received by adults in Australia was measured lower than 500 mm2 (Buonanno et. al., 2012c) and it is still not negligible when compared to the Italian population daily average alveolar surface area dose (about 2000 mm2) since most of the activities they performed during the day provide doses smaller than 20 mm2 (Buonanno et. al., 2011a; Buonanno et. al., 2012b). The authors want to point out that such significant dose was calculated considering a very short printing time (40 min): longer printing times are very common when larger or more complex models have to be printed, correspondingly increasing the dose received by people.

- Conclusions

In the present paper a comprehensive analysis of the particle emission from a 3D printer was assessed. In particular, a low-cost device was analyzed and different filament materials and printing temperatures were considered in the experimental campaign.

Particle number, alveolar-deposited surface area and PM fraction concentrations were continuously measured during the printing process as well as particle number size distributions. Particle emission rates and factors were calculated for all the tests performed.

Most of the materials and temperatures tested during the printing processes were recognized to emit sub-micron particles: in fact, particle number and alveolar-deposited surface area concentrations up to 1×106 part. cm-3 and 1×103 µm2 cm-3 were measured, respectively. On the contrary no contributions to the particle mass concentrations (PM1, PM2.5 and PM10) was recognized for all the tests performed. Particle number distribution measurements revealed a mode in the ultrafine range of the freshly-emitted particles (typically in the range 10-30 nm).

Particle number emission rates (factors) up to approximately 3×1012 particles min-1 (1×1011 particles mm-1) were measured. Particle emission was found to increase as function of the printing temperature: the authors speculate that such behavior is due to the higher material decomposition typically occurring at higher temperatures which lead to higher vapor pressure of organic material likely promoting the particle nucleation. As regards the PLA, which represents the most used and investigated materials, a negligible emission was measured for printing temperatures lower than 220 °C, whereas a particle emission rate of about 1×1011 was measured at 240 °C.

The high particle concentrations resulting from 3D printing activities also caused large alveolar-surface particle doses received by people residing in naturally ventilated rooms/offices: doses up to 200 mm2 were estimated showing the significant contribution of such activities on the daily dose. The authors point out that such findings could be useful in providing information on indoor particle sources whose use is becoming popular in private homes too.

References

Adams, K., Bankston, J., Barlow, A., Holdren, M.W., Meyer, J. and Marchesani, V.J. (1999) Development of Emission Factors for Polypropylene Processing, Journal of the Air & Waste Management Association, 49, 49-56.

Afshari, A., Matson, U. and Ekberg, L.E. (2005) Characterization of indoor sources of fine and ultrafine particles: a study conducted in a full-scale chamber, Indoor Air, 15, 141-150.

Al-Itry, R., Lamnawar, K. and Maazouz, A. (2012) Improvement of thermal stability, rheological and mechanical properties of PLA, PBAT and their blends by reactive extrusion with functionalized epoxy, Polymer Degradation and Stability, 97, 1898-1914.

Azimi, P., Zhao, D., Pouzet, C., Crain, N.E. and Stephens, B. (2016) Emissions of Ultrafine Particles and Volatile Organic Compounds from Commercially Available Desktop Three-Dimensional Printers with Multiple Filaments, Environmental Science & Technology, 50, 1260-1268.

Buonanno, G., Dell'isola, M., Stabile, L. and Viola, A. (2009a) Uncertainty budget of the SMPS-APS system in the measurement of PM 1, PM 2.5, and PM 10, Aerosol Science and Technology, 43, 1130-1141.

Buonanno, G., Dell'isola, M., Stabile, L. and Viola, A. (2010) Critical Aspects of the Uncertainty Budget in the Gravimetric PM Measurements, Measurement, 44, 139-147.

Buonanno, G., Fuoco, F.C., Marini, S. and Stabile, L. (2012a) Particle Resuspension in School Gyms during Physical Activities, Aerosol and Air Quality Research, 12, 803–813.

Buonanno, G., Giovinco, G., Morawska, L. and Stabile, L. (2011a) Tracheobronchial and alveolar dose of submicrometer particles for different population age groups in Italy, Atmospheric Environment, 45, 6216-6224.

Buonanno, G., Giovinco, G., Morawska, L. and Stabile, L. (2012b) Corrigendum to " Tracheobronchial and alveolar dose of submicrometer particles for different population age groups in Italy" [Atmos. Environ. 45 (2011) 6216-6224], Atmospheric Environment, 49, 423.

Buonanno, G., Giovinco, G., Morawska, L. and Wang, L. (2011b) Submicrometer Particle Dose for Different Population Age Groups in Brisbane, Australia, Metrology Society of Australia Conference, A Climate for Better Measurement Deakin Management and Convention Centre, Geelong (VIC). 19-21 October 2011.

Buonanno, G., Johnson, G., Morawska, L. and Stabile, L. (2011c) Volatility characterization of cooking-generated aerosol particles, Aerosol Science and Technology, 45, 1069-1077.

Buonanno, G., Morawska, L. and Stabile, L. (2009b) Particle emission factors during cooking activities, Atmospheric Environment, 43, 3235-3242.

Buonanno, G., Morawska, L. and Stabile, L. (2011d) Exposure to welding particles in automotive plants, Journal of Aerosol Science, 42, 295-304.

Buonanno, G., Morawska, L., Stabile, L., Wang, L. and Giovinco, G. (2012c) A comparison of submicrometer particle dose between Australian and Italian people, Environmental Pollution, 169, 183-189.

Chien, Y.-C., Liang, C., Liu, S.-H. and Yang, S.-H. (2010) Combustion Kinetics and Emission Characteristics of Polycyclic Aromatic Hydrocarbons from Polylactic Acid Combustion, Journal of the Air & Waste Management Association, 60, 849-855.

Chuang, H.-C., Jones, T. and Bérubé, K. (2012) Combustion particles emitted during church services: Implications for human respiratory health, Environment International, 40, 137-142.

Commission Regulation (2010) Commission Regulation (EU) No 453/2010 of 20 May 2010 amending Regulation (EC) No 1907/2006 of the European Parliament and of the Council on the Registration, Evaluation, Authorisation and Restriction of Chemicals (REACH), Vol. L 133/1, Official Journal of theEuropean Union.

Corsi, R.L., Siegel, J.A. and Chiang, C. (2008) Particle resuspension during the use of vacuum cleaners on residential carpet, J Occup Environ Hyg, 5, 232-238.

D’ambrosio Alfano, F.R., Dell’isola, M., Ficco, G. and Tassini, F. (2012) Experimental analysis of air tightness in Mediterranean buildings using the fan pressurization method, Building and Environment, 53, 16-25.

De Obaldia, E.E., Jeong, C., Grunenfelder, L.K., Kisailus, D. and Zavattieri, P. (2015) Analysis of the mechanical response of biomimetic materials with highly oriented microstructures through 3D printing, mechanical testing and modeling, Journal of the Mechanical Behavior of Biomedical Materials, 48, 70-85.

Destaillats, H., Maddalena, R.L., Singer, B.C., Hodgson, A.T. and Mckone, T.E. (2008) Indoor pollutants emitted by office equipment: A review of reported data and information needs, Atmospheric Environment, 42, 1371-1388.

European Parliament and Council of the European Union (2011) Directive 2011/65/EU of the European Parliament and of the Council of 8 June 2011

on the restriction of the use of certain hazardous substances in electrical and electronic equipment (recast), Vol. L 174/88, Official Journal of theEuropean Union.

Fissan, H., Neumann, S., Trampe, A., Pui, D.Y.H. and Shin, W.G. (2007) Rationale and principle of an instrument measuring lung deposited nanoparticle surface area, Journal of Nanoparticle Research, 9, 53-59.

Fuoco, F., Buonanno, G., Stabile, L. and Vigo, P. (2014) Influence parameters of particle concentration and size distribution in the mainstream of e-cigarettes, Environmental Pollution, 184, 523-529.

Fuoco, F., Stabile, L., Buonanno, G., Trassiera, C., Massimo, A., Russi, A., Mazaheri, M., Morawska, L. and Andrade, A. (2015) Indoor Air Quality in Naturally Ventilated Italian Classrooms, Atmosphere, 6, 1652.

Ghirga, G. and Pipere, M. (2012) Are children safe indoor from outdoor air pollution? A short review, Open Journal of Pediatrics, 2, 93-96.

Glasschroeder, J., Prager, E. and Zaeh, M.F. (2015) Powder-bed-based 3D-printing of function integrated parts, Rapid Prototyping Journal, 21, 207-215.

Hänninen, O., Brüske-Hohlfeld, I., Loh, M., Stoeger, T., Kreyling, W., Schmid, O. and Peters, A. (2010) Occupational and consumer risk estimates for nanoparticles emitted by laser printers, Journal of Nanoparticle Research, 12, 91-99.

He, C., Morawska, L., Hitchins, J. and Gilbert, D. (2004) Contribution from indoor sources to particle number and mass concentrations in residential houses, Atmospheric Environment, 38, 3405-3415.

He, C., Morawska, L. and Taplin, L. (2007) Particle emission characteristics of office printers, Environmental Science and Technology, 41, 6039-6045.

International Commission on Radiological Protection. (1994) Human respiratory tract model for radiological protection. A report of a Task Group of the International Commission on Radiological Protection., Annals of the ICRP, 24, 1-482.

Ishizuka, Y., Tokumura, M., Mizukoshi, A., Noguchi, M. and Yanagisawa, Y. (2010) Measurement of Secondary Products During Oxidation Reactions of Terpenes and Ozone Based on the PTR-MS Analysis: Effects of Coexistent Carbonyl Compounds, International Journal of Environmental Research and Public Health, 7, 3853-3870.

Jarmer, D.J., Lengsfeld, C.S. and Randolph, T.W. (2004) Nucleation and growth rates of poly(L-lactic acid) microparticles during precipitation with a compressed-fluid antisolvent, Langmuir : the ACS journal of surfaces and colloids, 20, 7254-7264.

Kim, Y., Gidwani, A., Wyslouzil, B.E. and Sohn, C.W. (2010) Source term models for fine particle resuspension from indoor surfaces, Building and Environment, 45, 1854-1865.

Kim, Y., Yoon, C., Ham, S., Park, J., Kim, S., Kwon, O. and Tsai, P.J. (2015) Emissions of Nanoparticles and Gaseous Material from 3D Printer Operation, Environ Sci Technol, 49, 12044-12053.

Lee, C.-W. and Hsu, D.-J. (2007) Measurements of fine and ultrafine particles formation in photocopy centers in Taiwan, Atmospheric Environment, 41, 6598-6609.

Lithner, D., Larsson, Å. and Dave, G. (2011) Environmental and health hazard ranking and assessment of plastic polymers based on chemical composition, Science of The Total Environment, 409, 3309-3324.

Liu, D.-L. and Nazaroff, W.W. (2001) Modeling pollutant penetration across building envelopes, Atmospheric Environment, 35, 4451-4462.

Maynard, A.D. and Zimmer, A.T. (2002) Evaluation of grinding aerosols in terms of alveolar dose: The significance of using mass, surface area and number metrics, Ann Occup Hyg, 46, 315-319.

Mitchell, M.R., Link, R.E., Yang, M.-H. and Lin, Y.-H. (2009) Measurement and Simulation of Thermal Stability of Poly(Lactic Acid) by Thermogravimetric Analysis, Journal of Testing and Evaluation, 37, 102271.

Mokhtar, M.-A., Jayaratne, R., Morawska, L., Mazaheri, M., Surawski, N. and Buonanno, G. (2013) NSAM-derived total surface area versus SMPS-derived “mobility equivalent” surface area for different environmentally relevant aerosols, Journal of Aerosol Science, 66, 1-11.

Morawska, L., Afshari, A., Bae, G.N., Buonanno, G., Chao, C.Y., Hanninen, O., Hofmann, W., Isaxon, C., Jayaratne, E.R., Pasanen, P., Salthammer, T., Waring, M. and Wierzbicka, A. (2013) Indoor aerosols: from personal exposure to risk assessment, Indoor Air, 23, 462-487.

Moroni, B. and Viti, C. (2009) Grain size, chemistry, and structure of fine and ultrafine particles in stainless steel welding fumes, Journal of Aerosol Science, 40, 938-949.

Mota, C., Puppi, D., Chiellini, F. and Chiellini, E. (2015) Additive manufacturing techniques for the production of tissue engineering constructs, Journal of Tissue Engineering and Regenerative Medicine, 9, 174-190.

Noh, K.-C. and Hwang, J. (2010) The Effect of Ventilation Rate and Filter Performance on Indoor Particle Concentration and Fan Power Consumption in a Residential Housing Unit, Indoor and Built Environment, 19, 444-452.

Occupational Safety and Health Administration (2012) Occupational Safety and Health Standards, Part 1910, Washington DC, US, Occupational Safety and Health Administration, Department of Labor

Raasch, J., Ivey, M., Aldrich, D., Nobes, D.S. and Ayranci, C. (2015) Characterization of polyurethane shape memory polymer processed by material extrusion additive manufacturing, Additive Manufacturing, 8, 132-141.

Salthammer, T., Schripp, T., Wientzek, S. and Wensing, M. (2014) Impact of operating wood-burning fireplace ovens on indoor air quality, Chemosphere, 103, 205-211.

Schripp, T., Wensing, M., Uhde, E., Salthammer, T., He, C. and Morawska, L. (2008) Evaluation of Ultrafine Particle Emissions from Laser Printers Using Emission Test Chambers, Environmental Science & Technology, 42, 4338-4343.

See, S.W. and Balasubramanian, R. (2011) Characterization of fine particle emissions from incense burning, Building and Environment, 46, 1074-1080.

Singh, O.P., Ahmed, S.M. and Abhilash, M. (2015) Modern 3D printing technologies: Future trends and developments, Recent Patents on Engineering, 9, 91-103.

Spilak, M.P., Frederiksen, M., Kolarik, B. and Gunnarsen, L. (2014) Exposure to ultrafine particles in relation to indoor events and dwelling characteristics, Building and Environment, 74, 65-74.

Stabile, L., Dell’isola, M., Frattolillo, A., Massimo, A. and Russi, A. (2016) Effect of natural ventilation and manual airing on indoor air quality in naturally ventilated Italian classrooms, Building and Environment.

Stabile, L., Frattolillo, A., Dell’isola, M., Massimo, A. and Russi, A. (2015a) Air Permeability of Naturally Ventilated Italian Classrooms, Energy Procedia, 78, 3150-3155.

Stabile, L., Fuoco, F.C. and Buonanno, G. (2012) Characteristics of particles and black carbon emitted by combustion of incenses, candles and anti-mosquito products, Building and Environment, 56, 184-191.

Stabile, L., Fuoco, F.C., Marini, S. and Buonanno, G. (2015b) Effects of the exposure to indoor cooking-generated particles on nitric oxide exhaled by women, Atmospheric Environment, 103, 238-246.

Stabile, L., Jayaratne, E.R., Buonanno, G. and Morawska, L. (2014) Charged particles and cluster ions produced during cooking activities, Science of The Total Environment, 497–498, 516-526.

Stabile, L., Ruggiero, A., Iannitti, G. and Buonanno, G. (2013a) Generation of ultrafine particles by high-velocity impact of metal projectiles on a metallic target, Journal of Aerosol Science, 55, 66-77.

Stabile, L., Vargas Trassierra, C., Dell’agli, G. and Buonanno, G. (2013b) Ultrafine particle generation through atomization technique: the influence of the solution, Aerosol and Air Quality Research, 13, 1667–1677.

Stanton, M.M., Trichet-Paredes, C. and Sánchez, S. (2015) Applications of three-dimensional (3D) printing for microswimmers and bio-hybrid robotics, Lab on a Chip - Miniaturisation for Chemistry and Biology, 15, 1634-1637.

Steinle, P. (2015) Characterization of emissions from a desktop 3D printer and indoor air measurements in office settings, J Occup Environ Hyg, 1-36.

Stephens, B., Azimi, P., El Orch, Z. and Ramos, T. (2013) Ultrafine particle emissions from desktop 3D printers, Atmospheric Environment, 79, 334-339.

Stephens, B. and Siegel, J.A. (2011) Comparison of Test Methods for Determining the Particle Removal Efficiency of Filters in Residential and Light-Commercial Central HVAC Systems, Aerosol Science and Technology, 46, 504-513.

Tibbits, S. (2015) What's Next?, 3D Printing and Additive Manufacturing, 2, 91-91.

Unwin, J., Coldwell, M.R., Keen, C. and Mcalinden, J.J. (2013) Airborne emissions of carcinogens and respiratory sensitizers during thermal processing of plastics, Ann Occup Hyg, 57, 399-406.

Wallace, L.A., Ott, W.R. and Weschler, C.J. (2015) Ultrafine particles from electric appliances and cooking pans: experiments suggesting desorption/nucleation of sorbed organics as the primary source, Indoor Air, 25, 536-546.

Wardoyo, A.Y.P., Santjojo, D.H. and Putri, I.I.H. (2012) Indoor Outdoor Ultrafine Particle Measurements in Lecture Rooms, International Journal of Basic & Applied Sciences, 12, 198-201.

Yang, J., Zhang, Y., Zheng, S., Huang, L., Chen, F., Fan, P. and Zhong, M. (2014) Probing structure–heterogeneous nucleation efficiency relationship of mesoporous particles in polylactic acid microcellular foaming by supercritical carbon dioxide, The Journal of Supercritical Fluids, 95, 228-235.

Yang, M.H. and Lin, Y.H. (2009) Measurement and Simulation of Thermal Stability of Poly(Lactic Acid) by Thermogravimetric Analysis, Journal of Testing and Evaluation, 37.

Tables

Table 1 –  Characteristics of the investigated 3D printer Prusa i3.

| Print size (X×Y×Z) | 20×20×18 cm |
| --- | --- |
| Minimum layer height | 0.06 mm |
| Maximal speed | 200 mm s-1 |
| Step size in X/Y axes | 10 μm |
| Nozzle diameter | 0.4 mm for 1.75 mm filaments |
| Maximum extrusion temperature | 240 °C |
| Glass base (non-heated) | 20×20×0.3 cm |
| Machine Dimension | 46×37×51 cm |
| Weight | 6.5 kg |
| Electronics | Arduino Mega 2560 and RAMPS 1.4 |
| Cartridge heater (voltage, power) | 12 V, 40 W |

Table 2 – Description, thermal and mechanical properties of the materials under investigation.

| Filament material | Description | Density (g cm-3) | Melting temperature (°C) | Decomposition temperature (°C) | Izod impact strength, notched (kJ m-2) | Izod impact strength, unnotched (kJ m-2) | Tensile strength (max.) (MPa) | Flexural modulus (GPa) | Extrusion temperature recommended (°C) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PLA | Biodegradable thermoplastic aliphatic polyester derived from corn starch. | 1.24 | 160 | >230 | 2.8 | 32 | 61.5 | 3.295 | 180-220 |
| WOOD 1 | Wood powder-filled (40% Recycled wood) PLA with proprietary additivation (antioxidant, pigment) | 0.93 | 200 | >270 | n.a. | n.a. | n.a. | n.a. | 190-240 |
| WOOD 2 | PLA containing 30% of recycled pine woodfibres | 1.15 | >155 | >230 | 4.2 | 19 | 46 | 3.93 | 195-220 |
| COPPER | Copper powder-filled PLA with proprietary additivation (antioxidant, pigment) | 4.00 | 160 | >240 | 5.5 | 10 | 25 | 7 | 160-230 |
| BAMBOO | PLA containing 20% of bamboo fibres | 1.19 | >155 | >230 | 3 | 22 | 46 | 3.6 | 195-220 |
| FLEX PLA | Soft and Bendable Polylactic Acid | 0.96 | 165 | 210-260 | n.a. | n.a. | n.a. | n.a. | 190-240 |
| CP | Copolyester (styrene-free) | 1.27 | 220 | >270 | n.a. | n.a. | n.a. | 2.1 | 220-240 |
| CP-CARBON | Copolyester (styrene-free) containing 20% of milled carbon fibres | 1.35 | 235 | >270 | 6 | 60 | 76 | 6.2 | 235-255 |
| NYLON | Nylon | 1.14 | 224 | >280 | n.a. | n.a. | 90 | 0.97 | 190-240 |
| NINJAFLEX® | Specially formulated thermoplastic polyurethane (TPU) material (patent pending technology) | 1.20 (bulk density=0.5) | 150 | >230 | n.a. | n.a. | 34.5 | n.a. | 210-225 |

n.a. = data not available

Table 3 – Summary of the tests performed for each material: printing temperatures, speeds and times, filament length/volume required, layer height.

| material | Printing temperature (°C) | Filament length/volume (mm)/(mm3) | Printing time (min) | Printing speed (mm/s) | Layer height (mm) |
| --- | --- | --- | --- | --- | --- |
| Zero test | 240 | No filament | 40 | 16 | 0.16 |
| PLA | 180, 200, 210, 220, 230, 240 | 1183/2845 |  |  |  |
| WOOD 1 | 220, 230, 240 |  |  |  |  |
| WOOD 2 | 230, 240 |  |  |  |  |
| COPPER | 220, 230, 240 |  |  |  |  |
| BAMBOO | 210, 220, 230, 240 |  |  |  |  |
| FLEX PLA | 240 |  |  |  |  |
| CP | 220, 230, 240 |  |  |  |  |
| CP-CARBON | 220, 230, 240 |  |  |  |  |
| NYLON | 220, 230, 240 |  |  |  |  |
| NINJAFLEX® | 220, 230, 240 |  |  |  |  |

Table 4 – Summary of particle number concentration peaks (Npeak, part. cm-3), alveolar-deposited particle surface area concentration peaks (Salv_peak, μm2 cm-3), and particle number distribution parameters (expressed as mode (nm)/GSD) measured for each test performed.

| Material | parameter | Printing temperature (°C) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | 180 °C | 200 °C | 210 °C | 220 °C | 230 °C | 240 °C |
| PLA | Npeak | negligible | negligible | negligible | (5.150.55)×103 | (8.213.27)×103 | (4.872.29)×104 |
|  | Salv_peak | negligible | negligible | negligible | (1.700.17)×101 | (1.890.22)×101 | (4.401.84)×101 |
|  | mode/GSD | negligible | negligible | negligible | 15.33.2/2.410.02 | 12.92.3/2.120.03 | 14.31.1/2.140.13 |
| WOOD 1 | Npeak | - | - | - | (1.450.88)×104 | (3.952.20)×104 | (9.271.95)×104 |
|  | Salv_peak | - | - | - | (2.641.60)×101 | (3.971.12)×101 | 8.303.32)×101 |
|  | mode/GSD | - | - | - | 12.52.4/2.550.01 | 16.94.5/2.160.22 | 17.13.0/1.810.10 |
| WOOD 2 | Npeak | - | - | - | - | (6.972.26)×105 | (9.512.45)×105 |
|  | Salv_peak | - | - | - | - | (4.591.01)×102 | (1.080.03)×103 |
|  | mode/GSD | - | - | - | - | 16.71.4/1.580.02 | 20.43.3/1.650.04 |
| COPPER | Npeak | - | - | - | (3.611.51)×105 | (4.533.37)×105 | (6.670.63)×105 |
|  | Salv_peak | - | - | - | (4.252.04)×102 | (5.644.91)×102 | (6.470.59)×102 |
|  | mode/GSD | - | - | - | 23.56.2/1.590.01 | 27.32.4/1.640.05 | 15.13.6/1.670.02 |
| BAMBOO | Npeak | - | - | (2.860.39)×104 | (1.110.02)×105 | (4.130.09)×105 | (9.543.83)×105 |
|  | Salv_peak | - | - | (5.730.29)×101 | (1.51.01)×102 | (3.730.01)×102 | (8.000.08)×102 |
|  | mode/GSD | - | - | 18.44.0/2.220.03 | 20.61.3/1.720.02 | 15.50.4/1.630.02 | 15.30.9/1.690.03 |
| FLEX PLA | Npeak | - | - | - | - | - | (2.350.39)×104 |
|  | Salv_peak | - | - | - | - | - | (3.320.13)×101 |
|  | mode/GSD | - | - | - | - | - | 18.60.3/2.26 0.03 |
| CP | Npeak | - | - | - | (8.930.74)×104 | (1.780.02)×105 | (5.620.85)×105 |
|  | Salv_peak | - | - | - | (9.59±1.85)×101 | (2.26±0.04)×102 | (6.16±2.26)×102 |
|  | mode/GSD | - | - | - | 16.14.1/2.090.07 | 19.90.1/1.740.03 | 15.82.4/1.610.09 |
| CP-CARBON | Npeak | - | - | - | (1.090.15)×105 | (2.300.44)×105 | (4.840.40)×105 |
|  | Salv_peak | - | - | - | (1.380.20)×102 | (2.280.22)×102 | (6.151.23)×102 |
|  | mode/GSD | - | - | - | 17.13.2/1.550.03 | 20.60.5/1.640.04 | 15.80.6/1.590.03 |
| NYLON | Npeak | - | - | - | negligible | (1.280.68)×104 | (1.410.28)×104 |
|  | Salv_peak | - | - | - | negligible | (2.230.15)×101 | (2.450.18)×101 |
|  | mode/GSD | - | - | - | negligible | 10.83.5/2.720.28 | 16.80.5/2.560.04 |
| NINJAFLEX® | Npeak | - | - | - | negligible | (1.781.03)×104 | (5.781.88)×104 |
|  | Salv_peak | - | - | - | negligible | (3.070.26)×101 | (4.231.30)×101 |
|  | mode/GSD | - | - | - | negligible | 16.49.2/2.570.12 | 14.33.0/2.050.22 |

Table 5 – Summary of particle number emission rate (particles min-1) and factor data (particles mm-1) measured for each test performed. Data in brackets refer to particle number emission factors.

| Material | Printing temperature (°C) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 180 °C | 200 °C | 210 °C | 220 °C | 230 °C | 240 °C |
| PLA | negligible (negligible) | negligible (negligible) | negligible (negligible) | (6.780.69)×109 ((2.260.23)×108) | (2.470.39)×1010 ((8.261.29)×108) | (9.980.54)×1010 ((3.331.81)×109) |
| WOOD 1 | - | - | - | (5.770.84)×1010 ((1.930.28)×109) | (1.690.67)×1011 ((5.652.23)×109) | (2.640.91)×1011 ((8.833.05)×109) |
| WOOD 2 | - | - | - | - | (1.911.07)×1012 ((6.383.57)×1010) | (2.781.04)×1012 ((9.293.47)×1010) |
| COPPER | - | - | - | (1.980.62)×1012 ((6.602.08)×1010) | (1.400.68)×1012 ((4.672.25)×1010) | (1.960.29)×1012 ((6.560.96)×1010) |
| BAMBOO | - | - | (1.651.08)×1010 ((5.523.61)×108) | (1.470.45)×1011 ((4.911.49)×109) | (5.840.11)×1011 ((1.951.95)×1010) | (2.651.76)×1012 ((8.845.87)×1010) |
| FLEX PLA | - | - | - | - | - | (4.181.77)×1010 ((1.400.59)×1010) |
| CP | - | - | - | (1.680.39)×1011 ((5.601.31)×109) | (3.200.09)×1011 ((1.070.03)×1010) | (1.580.69)×1012 ((5.282.32)×1010) |
| CP-CARBON | - | - | - | (2.310.41)×1011 ((7.731.36)×109) | (5.280.85)×1011 ((1.760.28)×1010) | (1.200.23)×1012 ((4.020.77)×1010) |
| NYLON | - | - | - | negligible (negligible) | (1.410.63)×1011 ((4.712.11)×109) | (1.550.33)×1011 ((5.191.10)×109) |
| NINJAFLEX® | - | - | - | negligible (negligible) | (6.822.37)×1010 ((2.280.79)×109) | (1.390.77)×1011 ((4.632.58)×109) |

Table 6 – Summary of alveolar surface area dose (mm2) received by an adult during a 40-min long 3D printing activity for each test performed.

| Material | Printing temperature (°C) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 180 °C | 200 °C | 210 °C | 220 °C | 230 °C | 240 °C |
| PLA | negligible | negligible | negligible | 3.940.42 | 5.100.62 | 12.084.96 |
| WOOD 1 | - | - | - | 6.704.58 | 8.922.04 | 19.996.96 |
| WOOD 2 | - | - | - | - | 108.0732.13 | 241.1544.71 |
| COPPER | - | - | - | 99.3043.44 | 124.6199.49 | 146.2711.20 |
| BAMBOO | - | - | 16.371.21 | 33.670.02 | 86.920.05 | 189.1840.71 |
| FLEX PLA | - | - | - | - | - | 9.730.42 |
| CP | - | - | - | 22.537.09 | 52.750.29 | 155.3096.90 |
| CP-CARBON | - | - | - | 43.303.41 | 44.741.85 | 130.4115.16 |
| NYLON | - | - | - | negligible | 5.310.66 | 5.840.42 |
| NINJAFLEX® | - | - | - | negligible | 8.640.82 | 10.482.89 |

Figure captions

Figure 1 – Examples of Minion Dave models printed through the investigated 3D printer Prusa i3.

Figure 2 – Particle number (N), Alveolar-deposited surface area (SAlv_dep), PM1, PM2.5 and PM10 concentration trends measured through the CPC 3775, NSAM 3550, and DustTrak 8534, respectively, during one of the three BAMBOO 220 °C tests.

Figure 3 – Particle number concentration trends measured through the CPC 3775 during one of the three (i) CP 220 °C test, (ii) CP 230 °C tests, and (iii) zero test.

Figure 4 – Particle number distribution trend measured through the SMPS 3936 during the BAMBOO 220 °C test corresponding to the CPC trend reported in Figure 2.

Figure 5 – Particle number emission rates as function of the extrusion temperature.